

**emco Bau**

Clean-off system CONFORM SE

|  |  |
| --- | --- |
| **Model** | CONFORM SE |
|  | For laying indoors |
| **Construction** | Tufting-Velours 1/8'' |
| **Pile above substrate** | 100% polyamide ECONYL |
| **Substrate material** | Polyester fleece |
| **Backing material** | Synthetic latex |
| **Pile weight / fibre weight** | 1200 g/m² |
| **Total weight (g/m²)** | 2400 g/m² |
| **Overall height (mm)** | 8.5 mm |
| **Combustion/fire behaviour** | Cfl-s1 |
| **Slip resistance** | DS (EN 13893) |
| **Certificates** | CE conformity EN 14041 (rolls only) |
| **Colours** | 76.01 Anthracite |
|  | 76.02 Beige |
|  | Mocha 76.03 |
|  | 76.04 Brown |
|  | 76.10 grey |
| **Colour fastness to artificial light ISO 105-B02** | ≥5 |
| **Colour fastness to rubbing ISO 105 X12** | ≥4 |
| **Colour fastness to water ISO 105 E01** | ≥4 |
| **Supplied as rolls SE/Bfl-s1** | 400 cm wide (no border) |
| **Product characteristics** | Soiling and moisture absorption |
| **Brand** | emco |
| **Dimensions** | Width:.........................m |
|  | Length:.........................m |
| **Contact** | emco Bautechnik GmbH · Memeler Straße 30 · D-42781 Haan · Germany · Tel.: +49 (0)21 29/34 75 80 · Telefax: +49 (0)21 29/34 75 810 · E-Mail: sauberlauf@emco.de · www.emco-bau.com |