emco Bau Logo

**emco Bau**

Non-slip underlay for textile underlay FLOCK

|  |  |
| --- | --- |
| **Model** | FLOCK |
|  | Non-slip underlay for textile floors |
| **Special colours** | Anthracite, grey flock |
| **Properties** | Effect with no adhesive |
|  | non-slip, dimensionally stable, absorbs the sound of footsteps, hard-wearing, easy to lay and cut |
| **Function** | The polyamide fibres of the flocked side of the material hook into the upper surface of the textile covering. |
| **Rolls (running metres)** | 20 m |
| **Width (cm)** | 80 cm |
|  | 120 cm |
|  | 180 cm |
| **Material structure** | PES/glass yarn fabric, coated on both sides, with special PVC paste polyamide flocking on the front, adhesion promoter on the back. |
| **Thickness** | approx. 2.5 to 3 mm |
| **Weight (g/m²)** | approx. 750 g/m² |
| **Brand** | emco |
| **Dimensions** | Width:.........................m |
|  | Length:.........................m |
| **Contact** | emco Bautechnik GmbH · Memeler Straße 30 · D-42781 Haan · Germany · Tel.: +49 (0)21 29/34 75 80 · Telefax: +49 (0)21 29/34 75 810 · E-Mail: sauberlauf@emco.de · www.emco-bau.com |