emco Bau Logo

**emco Bau**

Clean-off system INNOVA TILES

|  |  |
| --- | --- |
| **Model** | INNOVA TILES |
|  | For laying indoors |
| **Construction** | Tufting velour 5/32'' |
| **Pile above substrate** | 100% polyamide |
| **Substrate material** | Polyester fleece |
| **Backing material** | Bitumen |
| **Pile weight / fibre weight** | 850 g/m² |
| **Total weight (g/m²)** | 3930 g/m² |
| **Overall height (mm)** | 8 mm |
| **Combustion/fire behaviour** | Bfl-s1 |
| **Slip resistance** | DS (EN 13893) |
| **Certificates** | CE conformity EN 14041 (rolls only) |
| **Colours** | 36.01 black |
|  | 36.02 anthracite |
|  | 36.03 grey |
|  | 36.08 mocha |
|  | 36.10 slate |
| **Colour fastness to artificial light ISO 105-B02** | ≥5 |
| **Colour fastness to rubbing ISO 105 X12** | ≥4 |
| **Colour fastness to water ISO 105 E01** | ≥4 |
| **Supplied as tiles** | approx. 50 x 50 cm without a border (with asphalt coating) |
| **Product characteristics** | Soiling and moisture absorption |
| **Brand** | emco |
| **Contact** | emco Bautechnik GmbH · Breslauer Straße 34 - 38 · D-49808 Lingen (Ems) · Germany · Phone: +49 (0) 591/9140-500 · Fax: +49 (0) 591/9140-852 · Email: bau@emco.de · www.emco-bau.com |