

**emco Bau**

Clean-off system MAXIMUS® ASSISTANCE

|  |  |
| --- | --- |
| **Model** | MAXIMUS® ASSISTANCE |
|  | For laying indoors |
| **Construction** | Tufting-Velours 1/8'' |
| **Pile above substrate** | 100% polyamide |
| **Substrate material** | Polyester fleece |
| **Backing material** | Heavy coating |
| **Pile weight / fibre weight** | 1000 g/m² |
| **Total weight (g/m²)** | 3410 g/m² |
| **Overall height (mm)** | 11 mm |
| **Colours** | Black 80.01 |
|  | Black mottled 81.01 |
|  | Grey 80.03 |
| **Colour fastness to artificial light ISO 105-B02** | good 5-6 |
| **Colour fastness to rubbing ISO 105 X12** | good 5 |
| **Colour fastness to water ISO 105 E01** | good 5 |
| **Supplied as mats** | Mat max. 300 x 500 cm |
| **Product characteristics** | Soiling and moisture absorption |
| **Brand** | emco |
| **Dimensions** | Width:.........................m |
|  | Length:.........................m |
| **Contact** | emco Bautechnik GmbH · Memeler Straße 30 · D-42781 Haan · Germany · Tel.: +49 (0)21 29/34 75 80 · Telefax: +49 (0)21 29/34 75 810 · E-Mail: sauberlauf@emco.de · www.emco-bau.com |