emco Bau Logo

**emco Bau**

Clean-off system MAXIMUS®

|  |  |
| --- | --- |
| **Model** | MAXIMUS® |
|  | For laying indoors |
| **Construction** | Tufting-Velours 1/8'' |
| **Pile above substrate** | 100% polyamide |
| **Substrate material** | Polyester fleece |
| **Backing material** | Heavy coating |
| **Pile weight / fibre weight** | 1000 g/m² |
| **Total weight (g/m²)** | 3410 g/m² |
| **Overall height (mm)** | 9 mm |
| **Combustion/fire behaviour** | Bfl-s1 |
| **Slip resistance** | DS (EN 13893) |
| **Certificates** | CE conformity EN 14041 (rolls only) |
| **Colours** | 83.02 anthracite |
|  | 83.03 grey |
|  | 83.04 brown |
|  | 83.05 beige |
|  | 83.07 red |
|  | Black 80.01 |
|  | Black mottled 81.01 |
|  | Anthracite 80.02 |
|  | Anthracite mottled 81.02 |
|  | Grey 80.03 |
|  | Brown 80.04 |
|  | Brown mottled 81.04 |
|  | Red 80.07 |
| **Colour fastness to artificial light ISO 105-B02** | ≥5 |
| **Colour fastness to rubbing ISO 105 X12** | ≥4 |
| **Colour fastness to water ISO 105 E01** | ≥4 |
| **Bacterial reduction EHEC ASTM-e2149** | 29,4 % |
| **Bacterial reduction staphylococcus aureus ASTM-e2149** | 16,7 % |
| **Bacterial reduction klebsiella pneumoniae ASTM-e2149** | 68,2 % |
| **Supplied as rolls** | 130 cm wide (incl. border) |
|  | 200 cm wide (incl. border) |
| **Supplied as mats** | 60 x 90 cm (incl. border) |
|  | 90 x 150 cm (incl. border) |
|  | 130 x 200 cm (incl. border) |
| **Product characteristics** | Soiling and moisture absorption |
| **Brand** | emco |
| **Dimensions** | Width:.........................m |
|  | Length:.........................m |
| **Contact** | emco Bautechnik GmbH · Memeler Straße 30 · D-42781 Haan · Germany · Tel.: +49 (0)21 29/34 75 80 · Telefax: +49 (0)21 29/34 75 810 · E-Mail: sauberlauf@emco.de · www.emco-bau.com |