

**emco Bau**

Clean-off system ROYAL

|  |  |
| --- | --- |
| **Model** | ROYAL |
|  | For laying indoors |
| **Construction** | Tufting-Velours 1/8'' |
| **Pile above substrate** | 100% polyamide ECONYL |
| **Substrate material** | Polyester fleece |
| **Backing material** | Heavy coating |
| **Pile weight / fibre weight** | 1400 g/m² |
| **Total weight (g/m²)** | 4200 g/m² |
| **Overall height (mm)** | 11 mm |
| **Combustion/fire behaviour** | Bfl-s1 |
| **Slip resistance** | DS (EN 13893) |
| **Certificates** | CE conformity EN 14041 (rolls only) |
| **Colour fastness to artificial light ISO 105-B02** | ≥6 |
| **Colour fastness to rubbing ISO 105 X12** | ≥4 |
| **Colour fastness to water ISO 105 E01** | ≥4 |
| **Supplied as rolls** | 200 cm wide (incl. border) |
| **Product characteristics** | Soiling and moisture absorption |
| **Brand** | emco |
| **Contact** | emco Bautechnik GmbH · Breslauer Straße 34 - 38 · D-49808 Lingen (Ems) · Germany · Phone: +49 (0) 591/9140-500 · Fax: +49 (0) 591/9140-852 · Email: bau@emco.de · www.emco-bau.com |